## Slide 1
Institution of Permanent Way Engineers
“Study of possible causes of premature cracking of sleepers in Indian Railways”
Anupam Awasthi
Dy. CE/CON/Design & Drawing
ME/ University of Tokyo
Supervisor: Dr. Kohei Nagai
1
Notes: rs

## Slide 2
100 KM
Sleeper
The background
Cracking of PSC sleepers starts after 7-8 years.
2

## Slide 3
9 years old
12 years old
The problem of premature cracking of sleepers
Map Cracks at the ends
Longitudinal Cracks at middle
Cracking pattern indicates expansive reaction in concrete.
3
Longitudinal Cracks due to combined effect of expansion and pre-stress
Map Cracks without the effect of pre-stress
Top view

## Slide 4
Water
Water
C3A + Gypsum
Ettringite
Monosulfo-aluminate
Concrete
Reformation of Ettringite
Decomposition of
Primary Ettringite
Early age temp.
like steam curing
Moist Condition
T>70°C
Mechanism of Delayed Ettringite Formation
C3A
Primary
Ettringite
Delayed Ettringite
Early high temperature is a key factor for DEF problem.
4
Primary ettringite is good for the concrete
Delayed ettringite causes deleterious expansion
Delayed Ettringite
Primary ettringite
Steam curing for
early strength gain
Mechanism of Delayed Ettringite Formation
Aggregate
CHS gel
Ettringite
Ettringite
Ettringite
Ettringite

## Slide 5
Investigation of the problem of premature cracking
SEM & EDS
Countermeasures to avoid problem in future
Simulation of damage and evaluation of residual capacity
Objectives and flow of the study
TOOLS & METHODS
Damage SIMULATION
TOOLS & METHODS
Modification in manufacturing process
Overall strength improvement
1
2
3
EXPERIMENTS
5
XRF
Temperature measurement
ASR & DEF Simulation

## Slide 6
Investigation of the problem of premature cracking
SEM & EDS
Countermeasures to avoid problem in future
Simulation of damage and evaluation of residual capacity
Objectives and flow of the study
TOOLS & METHODS
Damage SIMULATION
TOOLS & METHODS
Modification in manufacturing process
Overall strength improvement
1
2
3
EXPERIMENTS
XRF
Temperature measurement
ASR & DEF Simulation

## Slide 7
Large ettringite deposition noticed in damaged sleepers.
6
SEM analysis of sleeper samples
1
Aggregate
CHS gel
Ettringite
CHS gel
Ettringite
Severely damaged
Undamaged
Aggregate
CSH gel
9 years old
Severely damaged
Moderately damaged
12 years old
21 years old
Undamaged
9 years old
40 Samples of concrete sleepers representing different damage level is collected from India
Ettringite
Enlarged view
Damaged sleeper samples shows large ettringite deposits whereas good sleeper sample does not
Ettringite
Aggregate
Past study of DEF (Thomas et al., 2008)

## Slide 8
Al K
SiK
S K
CaK
keV
1.00
2.00
3.00
4.00
5.00
6.00
7.00
8.00
9.00
Synthesised ettringite
EDS pattern of spot
10
Specimen for EDS
CSH gel
Aggregate
Ettringite
1.1
2.1
3.1
4.1
5.1
6.1
7.1
Al K
SiK
S K
CaK
keV
EDS pattern of spot: ettringite
SEM Image
EDS analysis of sleeper samples
1
EDS analysis confirms the composition of DEF
7
These three indicates ettringite
Synthesised ettringite used for comparison

## Slide 9
Maximum curing temperature 75°C may trigger DEF
Steam
Sleeper
75 °C
STEAM CHAMBERS
Early high temperature of concrete is very important factor for DEF
8
Steam pipes
Curing tank
Steam chamber
Thin wall
Temperature measurement in India
Thermocouples
Data logger
Temperature rise during steam curing
1

## Slide 10
Maximum Inside temperature = 84.9 °C
Temperature rise inside the concrete 84.9 °C, is very critical for DEF.
Temperature measurement in India
1
9
Results of field measurement of temperature
Temperature inside concrete
Temperature outside concrete
Cooling cycle is excessively prolonged
Set curing cycle
Critical temperature for DEF

## Slide 11
Investigation of the problem of premature cracking
SEM & EDS
Countermeasures to avoid problem in future
Simulation of damage and evaluation of residual capacity
Objectives and flow of the study
TOOLS & METHODS
Damage SIMULATION
TOOLS & METHODS
Modification in manufacturing process
Overall strength improvement
1
2
3
EXPERIMENTS
XRF
Temperature measurement
ASR & DEF Simulation

## Slide 12
Countermeasures for pre-mature cracking
Maximum concrete temperature below 70°C is safe for DEF problem
3
Limit the maximum temperature inside the concrete below 70°C.
Trial curing cycles may be conducted to decide optimum
temperature.


10
Critical temperature for DEF
Example of trial curing cycle
Expected temperature inside the concrete
De-moulding strength = 40 MPa

## Slide 13
Countermeasures for pre-mature cracking
3
Bending cement with silica fume or slag to
improve interface characteristics

24
SEM image showing damage in interface
Aggregate
Other countermeasures proposed for overall improvement
Silica fume provide extra silica required for the hydration
11
Provision of extra reinforcement like
stirrups & spiral reinforcement at inserts

Stirrups provide confinement to the core concrete and resist expansive forces
Spiral reinforcement can resist failure at inserts

## Slide 14
Conclusions
Unique feature of the study: direct practical application of the results and findings.
12
Investigation reveals large ettringite deposition in the damaged sleepers of Indian Railways
Field measurement of temperature reveals that sleepers experiences high early age temperature (> 80°C ), which is very critical for DEF problem to occur in future
Investigations
1
Simulation
2
Countermeasures
3
Pre-stress is successfully introduced in RBSM model
Structural scale simulation of cracking pattern does not yield localised longitudinal cracks observed in field
Material scale simulation of ASR agrees well with the field observation but DEF does not indicating other mechanism might be taking place in concrete
Countermeasure is suggested to limit maximum concrete temperature up to 70°C.
Blending cement with slilica fume or slag can improve interface characteristics
Stirrups and extra spiral reinforcement around insert can improve overall strength

## Slide 15
Thank you very much for your kind attention
The research work is selected for “Furuichi Award-2016” by the University of Tokyo which is given for best masters thesis.
The research work has been presented at “Asian Concrete Federation-2016” meet at Hanoi, Veitnam
Two International publications of research work:
1. Anupam Awasthi, Kohei Nagai, Shingo Asamoto and Seishi Goto, “Study of possible causes of premature cracking of sleepers in Indian Railways”, Asian Concrete Federation,2016 conference proceeding – abstracts p 86.
2. Liyanto Eddy, Anupam Awasthi, Koji Matsumoto, Kohei Nagai and Shingo Asamoto Mesoscopic, “Analysis of different expansion causes in concrete by 3D Rigid Body Spring Model” New Technologies for Urban Safety of Mega Cities in Asia, November 2016, Tacloban, Philippines
Previous publications…
13
anupamawasthi1978@gmail.com(Mob:9752440219)
Notes: rs

## Slide 16: Appendix

## Slide 17
Investigation of the problem of premature cracking
SEM & EDS
Countermeasures to avoid problem in future
Simulation of damage and evaluation of residual capacity
Objectives and flow of research
TOOLS & METHODS
Damage SIMULATION
TOOLS & METHODS
Modification in manufacturing process
Overall strength improvement
1
2
3
EXPERIMENTS
5
XRF
Temperature measurement
ASR & DEF Simulation

## Slide 18
Chart: 
 | 200 | 100
Chart: 
| 2005 | Severely damaged
Compressive Strength of core (MPa) | 115.4 | 34.65
Damaged sleeper shows considerable reduction of strength
Residual capacity of sleepers
2
Static Bending Test
Compressive Strength Test
10
Severely damaged
Undamaged
Bending capacity (KN)
50%
100%
Severely damaged
Undamaged
Severely damaged
Undamaged
51%
170%
Percentage of 15 days target mean strength = 67.86 MPa
Compressive strength (MPa)
Undamaged
Severely damaged

## Slide 19
Simulation of damage by discrete analysis
2
Structural scale simulation is performed by RBSM
11
Predicted failure pattern
1
2
3
Top Surface
1
2
3
Observed failure pattern
Y
X
Z
Front face
Concrete element
PC strands
Y
X
Z
1375mm
Section at middle
Section of model at the ends
Section of model at the middle
Structural scale simulation
Material scale simulation
Concrete
Steel
Mortar
Aggregate
2750
235
RBSM is very effective for simulation of cracking pattern in concrete
Dimensions of the sleeper (mm)
150
270

## Slide 20
Simulation of pre-stress
19
2
Variable initial strain is introduced to steel elements
Variable stress in concrete at the ends representing transfer length
Compressive stress
Tensile stress
Chart: Distance from end of sleeper, mm
| 0 | 125 | 375 | 625 | 875 | 1125 | 1375 | 1625 | 1875 | 2125 | 2375 | 2625 | 2750
 | 0 | 2.5294 | 7.9007 | 10.7994 | 10.6858 | 10.2026 | 10.0037 | 10.2595 | 10.6573 | 10.771 | 7.7018 | 2.4441 | 0
Bottom elements
Stress at bottom fiber
Transfer length, Lt
Transfer length, Lt
εi
εi
Steel
Concrete
Pre-stressing force in sleeper is introduced successfully
Transfer length (Lt ) is the length required at the ends of pre-tensioned member for the build up of stress in concrete
Input initial strain
Tensile stress induced by initial strain
12

## Slide 21
Simulation of expansion in concrete
2
Simulation does not produce localised cracks in the middle portion
13
Actual case, Ends
20%
Simulation result, Ends
Simulation result, Middle
Actual case, Middle
Pre-stress
Simulation of 20% expansion of random faces is conducted after pre-stress
Simulation of smaller material scale is necessary to pin point the problem
=> Content of paste in the concrete ~ 23%

## Slide 22
2
150mm
150 mm
150mm
150mm
150mm
150mm
Chart: Aggregate Size (mm)
| 0 | 4 | 5 | 6 | 8 | 10 | 12 | 14 | 16 | 18 | 20 | 22 | 24 | 26
 | 0 | 8 | 11 | 19 | 38 | 55 | 65 | 74 | 82 | 91 | 100 | 100 | 100 | 100
 | 0 | 0 | 0 | 4 | 12 | 21 | 34 | 49 | 62 | 77 | 90 | 94 | 98 | 100
 | 0 | 0 | 0 | 14.7 | 29.4 | 42.4 | 55.4 | 68.4 | 81.4 | 91.4 | 100 | 100 | 100 | 100
: JSCE
: Analysis
Material scale simulation of DEF and ASR
2
DEF: mortar face expansion, ASR: aggregate interface expansion
Mortar model
Aggregate model
14
Mechanism of ASR
Mechanism of DEF
Random expanding aggregates
Random expanding mortar faces
Ettringite
ASR gel
ASR gel
Simulation of DEF expansion
Simulation of ASR expansion

## Slide 23
Simulation of ASR and DEF
2
Other mechanism may take place in case of DEF damage in concrete
Mortar Expansion (DEF)
Internal stress
DEF damage
Simulation, 25% mortar expansion
Actual cracking pattern
Crack view
15
Simulation, 25% aggregate expansion
Crack view
Internal stress
Actual cracking pattern
Aggregate Interface Expansion (ASR)
ASR damage
Crystal Growth Theory  Another mechanism of DEF: cracks are caused by the pressure at the interface
Based on Paste Expansion Theory cracks are caused by only expansion in cement paste
Matching
Not Matching

## Slide 24
Steam Chambers
Cover
Steam
Rising steam
Temperature measurement in India
Three sleepers are selected for temperature measurement
1
13
Steam Chamber
Steam pipes
Curing tank
Data logger
Arrangement of curing chambers
Thin wall

## Slide 25
Temperature measurement in India
1
9
Area depicts heat energy
Thin wall

Workers issue

Effect of Thin wall
Workers issue and thin wall of curing chamber affects cooling curve
16

## Slide 26
DEF
ESA
ISA
Traditional sulphate attack
New phenomenon detected in 1980s in Railway sleepers
Traditional approach
Destruction of primary ettringite> reformation when exposed to water > influence of ASR
Holistic approach
?

## Slide 27: Portland Cement Association

## Slide 28
New Good Sleeper, 2012
Old Good Sleeper, 1992
Relatively New Cracked Sleeper, 2005
Relatively New Cracked Sleeper, 2005
80%
170%
65.4%
51%
Comparison to mean strength 67.86 N/mm2
Notes: New good: 7A OCS 12RT 2496 1393 19.7.12
Old good: OCAL 92 32 A A-12 52 Kg Balod
Relatively New Cracked Sleeper: RCS 05 4183 303D Wide Gauge Curve Sleeper
Relatively New Cracked Sleeper: RCS 05 4183 314 Wide Gauge Curve Sleeper

## Slide 29: Comparison of Cement and Process of steam curing
Parameters | Unit | As per IS 12269-1987 for Early High Strength cement | Indian Sleeper plant values | Composition at which problem of DEF Noticed in European countries | New German Guidelines issued to solve the problem of DEF | Japanese sleepers Plant Values
SO3 | % | 3.5 max | 2.22-2.35 | 4 |  | 2.96 (Max 3.08)
C3A | % | 10 max | 7.5-8.04 | 8 | 12 | 
Fineness | Sq m /kg | 370 min | 375.7-380.3 | 460-480 |  | 441 (SD 91)
Cement Content | Kg/cum |  | 453.17 | 400 |  | 448
W/C ratio |  |  | 0.33 | 0.36-0.39 |  | 0.342
Delay period | Hrs |  | 2.0 | 1-2 | 4 | 3
Max Temperature | °C |  | 75 | 75-80 | 60 | 50
Soaking period | Hrs |  | 9.5 | 2.5-4.0 |  | 
One day Strength | MPa |  | 42.89 | 43-56 | 68 | 40
Rate of Temp rise | °C/ Hr |  | 16 |  | 10-15 | 15
Max size of aggregate | mm |  | 20 |  | 16 | 20
Yellow Colour shows the venerable values in case of Indian PSC sleepers which may cause damage

## Slide 30
  SEM differences
ASR
DEF

## Slide 31: SEM image
Aggregate
Aggregate
C-H-S gel
old Good sleeper

## Slide 32: Close up sem image
Aggregate
C-H-S gel
old Good sleeper

## Slide 33: EDS image & results
Element | [wt.%] | [norm. wt.%] | [norm. at.%] | Compound | [norm. wt.%] | Error in wt.% (3 Sigma)
Oxygen | 19.6002 | 36.71020563 | 56.75379207 |  | 1.84637E-15 | 6.741330188
Aluminium | 0.50419302 | 0.944328608 | 0.865701493 | Al2O3 | 1.784274613 | 0.15129767
Sulfur | 0.12394375 | 0.232140516 | 0.17906797 | SO3 | 0.579621552 | 0.093346849
Calcium | 25.3718022 | 47.52013126 | 29.32806097 | CaO | 66.49047878 | 2.344241111
Silicon | 7.70930108 | 14.43913982 | 12.71659788 | SiO2 | 30.89016071 | 1.040181606
Magnesium | 0.08225213 | 0.154054168 | 0.156779611 | MgO | 0.255464341 | 0.093411144
Sum: | 53.3916921 | 100 | 100 |  |  | 
Bruker Nano GmbH, Germany |  |  |  | 2015/08/31
 | Quantax |  |  | 
Results | 1015 |  |  | 
Date: | 2015/08/31 |  |  | 
old Good sleeper

## Slide 34: Specimen of More damaged sleeper
More damaged sleeper manufactured in 2002

## Slide 35: SEM IMAGE -1
More damaged sleeper
Aggregate
Large deposition of ettringite
Ettringite
Ettringite

## Slide 36: Close up
More damaged sleeper
Aggregate
Ettringite
C-H-S gel

## Slide 37: SEM IMAGE -2
Large ettringite deposit
C-H-S gel
C-H-S gel
More damaged sleeper

## Slide 38: Close up
Ettringite (needle like structure )
More damaged sleeper

## Slide 39: EDS image & results
Element | [wt.%] | [norm. wt.%] | [norm. at.%] | Compound | [norm. wt.%] | Error in wt.% (3 Sigma)
Sulfur | 8.563695 | 12.64118 | 9.356461 | SO3 | 31.5632 | 0.998346
Calcium | 26.04977 | 38.453 | 22.77158 | CaO | 53.80369 | 2.426149
Aluminium | 5.246524 | 7.744583 | 6.812401 | Al2O3 | 14.63311 | 0.821572
Oxygen | 27.88445 | 41.16124 | 61.05956 |  | -1.9E-15 | 9.972725
Sum: | 67.74444 | 100 | 100 |  |  | 
More damaged sleeper
Bruker Nano GmbH, Germany |  |  |  | 2015/08/31
 | Quantax |  |  | 
Results | sleeper1.spx |  |  | 
Date: | 2015/08/31 |  |  | 

## Slide 40: Specimen of less damaged sleeper
less damaged sleeper manufactured in 2005

## Slide 41: SEM IMAGE -1
Ettringite
less damaged sleeper

## Slide 42: EDS image & results
Element | [wt.%] | [norm. wt.%] | [norm. at.%] | Compound | [norm. wt.%] | Error in wt.% (3 Sigma)
Oxygen | 28.4734 | 41.03691 | 60.98522 |  | 5.86E-18 | 10.29794
Aluminium | 5.228539 | 7.535562 | 6.640527 | Al2O3 | 14.23817 | 0.819253
Sulfur | 8.725868 | 12.57604 | 9.325086 | SO3 | 31.40057 | 1.015624
Calcium | 26.95705 | 38.85149 | 23.04917 | CaO | 54.36126 | 2.507154
Sum: | 69.38486 | 100 | 100 |  |  | 
less damaged sleeper
Bruker Nano GmbH, Germany |  |  |  | 2015/08/31
 | Quantax |  |  | 
Results | 1013 |  |  | 
Date: | 2015/08/31 |  |  | 

## Slide 43: SEM IMAGE -2
less damaged sleeper
Ettringite
C-H-S gel
C-H-S gel
C-H-S gel
Aggregate

## Slide 44: Close up
less damaged sleeper
Ettringite (needle like structure )

## Slide 45: EDS image & results
Element | [wt.%] | [norm. wt.%] | [norm. at.%] | Compound | [norm. wt.%] | Error in wt.% (3 Sigma)
Oxygen | 35.64355 | 47.60912 | 64.32635 |  | 1.53E-15 | 13.06488
Aluminium | 3.175559 | 4.241597 | 3.398327 | Al2O3 | 8.014343 | 0.538584
Sulfur | 4.906416 | 6.553504 | 4.418056 | SO3 | 16.36316 | 0.620333
Calcium | 13.51907 | 18.05743 | 9.739853 | CaO | 25.26608 | 1.322536
Silicon | 17.62247 | 23.53835 | 18.11742 | SiO2 | 50.35642 | 2.290259
Sum: | 74.86706 | 100 | 100 |  |  | 
less damaged sleeper
Bruker Nano GmbH, Germany |  |  |  | 2015/08/31
 | Quantax |  |  | 
Results | 1012 |  |  | 
Date: | 2015/08/31 |  |  | 

## Slide 46: Curing
Max temp 75°C
After steam curing water curing for 14 days
Separate Steam chambers
Max temp 50°C
No water curing
Steam brought through pipes at the place of casting
INDIAN
JAPANESE

## Slide 47
JAPANESE SLEEPER PLANT Pipe line carrying steam for curing

## Slide 48
JAPANESE SLEEPER PLANT curing in situ in long line

## Slide 49
INDIAN SLEEPER PLANT Curing chambers

## Slide 50: Reinforcement
No extra reinforcement other than pre-stressing tendons
Tendons are not ribbed
Only pre-tensioned
Stress bench method
Extra reinforcement near insert and extra transverse reinforcement
Ribbed tendons
Both pre and post tensioned
Long line method
INDIAN
JAPANESE

## Slide 51
JAPANESE SLEEPER PLANT Extra helical reinforcement around insert and extra transverse reinforcement

## Slide 52
JAPANESE SLEEPER PLANT Ribbed tendons

## Slide 53
JAPANESE SLEEPER PLANT Both post- tensioned and pre-tensioned

## Slide 54
INDIAN SLEEPER PLANT stress bench method
JAPANESE SLEEPER PLANT long line method

## Slide 55: Strength Testing
Only bending test
Bending test and Insert pulling test
INDIAN
JAPANESE

## Slide 56
INDIAN SLEEPER PLANT Bending test

## Slide 57
JAPANESE SLEEPER PLANT Bending and Insert pulling tests

## Slide 58: Concreting
Weigh batching automatic but not computerised
Advanced and Computerised batching plant
INDIAN
JAPANESE

## Slide 59
INDIAN SLEEPER PLANT concrete mixing & placing

## Slide 60
JAPANESE SLEEPER PLANT concrete mixing & placing

## Slide 61: Special mortar application at the face
Only bituminous painting and no mortar
Special mortar is applied
INDIAN
JAPANESE

## Slide 62
JAPANESE SLEEPER special mortar curing
INDIAN SLEEPER No mortar curing at the end

## Slide 63: Heavier section
Total weight 270 Kg
Total weight 300 kg
INDIAN
JAPANESE

## Slide 64
JAPANESE SLEEPER DESIGN for Shinkansen Standard Gauge 1435 mm
INDIAN SLEEPER DESIGN for Broad Gauge 1673 mm

## Slide 66: Delayed ettringite formation in Swedish concrete railroad ties
Unexpected, steam curing < 60°C
Produced between 1992 to 1996
Map cracking in 1999

## Slide 67
Samples
  Cracked
  Uncracked
Examination
  Visual and stereo optical microscopy
  Scanning Electron Microscope with EDS
Nature of crack or sign of deposit
Examination of deposit